Baseline parameters – 05/27/2005

Eurisol-DS task #3 “100kW direct target station”

| Parameter | Symbol | Units | Nval | Range |
| --- | --- | --- | --- | --- |
| Target material | Ztarg | - | SiC, Ta, BeO, Pb (molten) | UCx, MgO |
| Beam particles | Zbeam | - | Proton | Deuterium – 12C |
| Beam particle energy | Ebeam | GeV | 1 | 0.5 – 3 |
| Beam current | Ibeam | A | 100 | 100 – 1000 |
| Beam time structure | - | - | dc | ac 50Hz 1ms pulse |
| Gaussian beam geometry | σbeam | mm | 7 | 3 – 20 |
| Beam power | Pbeam | kW | 100 | 100-1000 |
| Target thickness | X | g/cm2 | 200 | 10 – 250 |
| Target radius (cylinder) | rtarg | mm | 3σbeam | 3σbeam – 5σbeam |
| Target temperature | Ttarg | ºC | 2000 | 500-2500 |
| Number of target containers | jtarg | - | 4 | 1 – 10 |
| Plasma ionization outlet diameter | Øout | mm | 3 | 2 – 6 |

Edited by T. Stora for the EurisolDS-T3 CERN work group.

Letter to the Task leaders:

Dear colleagues,

You will find attached the table of baseline parameters useful in the framework of the EurisolDS-task #3 “100 kW direct station”.

It comprises for each of the parameters:

symbol

units

nominal value

range of  values.

It will be updated periodically according to the progress of our task, on a yearly basis (with a possible early review for this 1st year).

Investigations within our task are only planned at nominal values. Additional investigations could be envisaged by changing the value of a parameter within its range, while keeping the others at their nominal value.

With our best regards,

Thierry Stora, on behalf of the EurisolDS-T3 CERN work group.